**TECHNICAL DATA SHEET**

***R730 Sprazinc***

***Protective zinc paint***

**Light** coloured cold zinc paint; mono-component with high molecular weight; ideal to retouch galvanised parts; it withstands greases and oils; dries quickly and can be used as primer for any type of varnish.

**Available as spray**.

**APPLICATION AREAS:**

widely used for the **anti-corrosive protection** of metal products exposed to the elements and the aggressive action of industrial atmospheres. It guarantees effective protection.

**USE:**

apply the product in the most appropriate way.

**Spray FEATURES**

* Appearance: light grey liquid
* Odour: characteristic
* Flash point: below 0°C
* Relative density: about 0.95 gr/ml
* % dry residual zinc: 5%
* % Zinc in weight on the total: 2%
* Purity and quality: 100% superfine
* Drying at 20°C: (dry dust free) 3-5 minutes / (in depth) 8-12 hours
* Covering power about 1 m2 (400 ml)
* Water solubility: insoluble
* Lipid solubility: soluble